EN 10149-2 S315MC steel plate/sheet for High yield strength cold forming steel

Key words: S315MC steel plate/sheet, EN 10149-2 S315MC steel plate/sheet, S315MC steel plate/sheet supplier/Chinese supplier, S315MC steel plate/sheet price, S315MC steel plate/sheet mechanical property.

EN 10149-2 S315MC steel equivalent grade:
S315MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.0972. The equivalent grades of S315MC steel are NFA 36-231 E 315 D, BS 1449 HR 43F35.

| S315MC EN 10149-2 Material #: 1.0972 | Comparison of steel grades |
| --- | --- |
|  | NFA 36-231 | E 315 D |
|  | BS 1449 | HR 43F35 |

EN 10149-2 S315MC steel chemical composition %:
Main chemical composition in EN 10149-2 S315MC steel is carton max 0.19, silicon max 0.55, manganese max 1.6, phosphorus max 0.035, Sulphur max 0.035. More detailed information about S315MC steel, please refer to the down table:

| Chemical analysis -% by mass* | C | Si | Mn | P | S 1) | Altotal | Mo | Ti | B |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | max. | max. | max. | max. | max. | min. | max. | max. | max. |
|  | 0,12 | 0,50 | 1,30 | 0,025 | 0,020 | 0,015 | - | 0,15 | - |

EN 10149-2 S315MC steel mechanical property:
EN10149-2 S315MC is a technical delivery conditions for high yield strength cold forming steels.It is according to EN10149-2 standard.we can regard S315MC steel plates/sheets are low-perlite steel grades offer excellent bending, flanging, cold-borderingand folding properties in both longitudinal and transverse direction. The bending radii specified below should be observed as minimum values.

| Mechanical properties | Yield Strength ReH [N/mm2] t ransv.min. | Tensile Strength Rm [N/mm2] transv. | Min.totalel ongation [%] | Smallest recom mended bending radius bending angles ≤ 90 |
| --- | --- | --- | --- | --- |
| S315MC | 315 | 390 - 510 | L0 = 80 mm | L0= 5,65 √S0 | e1) ≤ 3 | 3 < e1)< 6 | e1) > 6 |
|  |  |  | e2) < 3 | e2) ≥ 3 | 0,25 e | 0,5 e | 1,0 e |
|  |  |  | 20 | 24 |  |  |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S315MC steel are available, so if need, welcome to contact ICE steel sales team.