EN 10149-2 S355MC steel plate/sheet for High yield strength cold forming steel

Key words: S355MC steel plate/sheet, EN 10149-2 S355MC steel plate/sheet, S355MC steel plate/sheet supplier/Chinese supplier, S355MC steel plate/sheet price, S355MC steel plate/sheet mechanical property.

EN 10149-2 S355MC steel equivalent grade:
S355MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.0976. The equivalent grades of S355MC steel are SEW092 QStE 380TM, NFA36-231 E355D, UNI8890 FeE355TM, ASTM 050XLK.

| S355MC EN 10149-2 Material #: 1.0976 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 380TM |
|  | NFA36-231 | E355D |
|  | UNI8890 | FeE355TM |
|  | ASTM | 050XLK |

EN 10149-2 S355MC steel chemical composition %:
Main chemical composition in EN 10149-2 S355MC steel is carton max 0.12, silicon max 0.50, manganese max 1.5, phosphorus max 0.025, Sulphur max 0.02. More detailed information about S355MC steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S355MC | 0.12 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.09 | 0.2 | 0.15 |

EN 10149-2 S355MC steel mechanical property:

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 |

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 |

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 19 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S355MC steel are available, so if need, welcome to contact ICE steel sales team.