EN 10149-2 S420MC steel plate/sheet for High yield strength cold forming steel

Key words: S420MC steel plate/sheet, EN 10149-2 S420MC steel plate/sheet, S420MC steel plate/sheet supplier/Chinese supplier, S420MC steel plate/sheet price, S420MC steel plate/sheet mechanical property.

EN 10149-2 S420MC steel equivalent grade:
S420MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.0972. The equivalent grades of S420MC steel are SEW092 QStE 420TM, NFA36-231 E420D, UNI8890c FeE420TM, ASTM 060XLK, BS1449 HR50F45.

| S420MC EN 10149-2 Number:1.0980 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 420TM |
|  | NFA36-231 | E420D |
|  | UNI8890 | FeE420TM |
|  | ASTM | 060XLK |
|  | BS1449 | HR50F45 |

EN 10149-2 S420MC steel chemical composition %:
Main chemical composition in EN 10149-2 S420MC steel is carton max 0.12, silicon max 0.50, manganese max 1.6, phosphorus max 0.025, Sulphur max 0.015. More detailed information about S420MC steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420MC | 0.12 | 0.50 | 1.6 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

EN 10149-2 S420MC steel mechanical property:

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 420 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 480-620 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 19 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 19 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S420MC steel are available, so if need, welcome to contact ICE steel sales team.