EN 10149-2 S460MC steel plate/sheet for High yield strength cold forming steel

Key words: S460MC steel plate/sheet, EN 10149-2 S460MC steel plate/sheet, S460MC steel plate/sheet supplier/Chinese supplier, S460MC steel plate/sheet price, S315460 steel plate/sheet mechanical property.

EN 10149-2 S460MC steel equivalent grade:
S420MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.0982. The equivalent grades of S460MC steel are SEW092 QStE 460TM, UNE AE440HC, AFNOR E455D, ASTM Gr.65, BS 50F45.

| S460MC EN 10149-2 Material #: 1.0982 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 460TM |
|  | UNE | AE440HC |
|  | AFNOR | E455D |
|  | ASTM | Gr.65 |
|  | BS | 50F45 |

EN 10149-2 S460MC steel chemical composition %:
Main chemical composition in EN 10149-2 S460MC steel is carton max 0.12, silicon max 0.50, manganese max 1.6, phosphorus max 0.025, Sulphur max 0.015. More detailed information about S460MC steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S460MC | 0.12 | 0.50 | 1.6 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.15 |

EN 10149-2 S460MC steel mechanical property:

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 460 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 520-670 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 14 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S460MC steel are available, so if need, welcome to contact ICE steel sales team.