EN 10149-2 S600MC steel plate/sheet for High yield strength cold forming steel

Key words: S600MC steel plate/sheet, EN 10149-2 S600MC steel plate/sheet, S600MC steel plate/sheet supplier/Chinese supplier, S600MC steel plate/sheet price, S600MC steel plate/sheet mechanical property.

EN 10149-2 S600MC steel equivalent grade: S600MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.8969. The equivalent grades of S600MC steel are SEW092 QStE 600TM, NFA36-231 E620D, BS1449 68F62.

| S600MC EN 10149-2 Material #:1.8969 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 600TM |
|  | NFA36-231 | E620D |
|  | BS1449 | 68F62 |

EN 10149-2 S600MC steel chemical composition %: 
Main chemical composition in EN 10149-2 S600MC steel is carton max 0.12, silicon max 0.50, manganese max 1.9, phosphorus max 0.025, Sulphur max 0.015. More detailed information about S600MC steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max | Mo max | B max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S600MC | 0.12 | 0.50 | 1.9 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.22 | 0.5 | 0.005 |

EN 10149-2 S600MC steel mechanical property:

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 600 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 650-820 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 13 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 11 |

ICE steel is the professional Chinese steel exporter, especially in fine-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S600MC steel are available, so if need, welcome to contact ICE steel sales team.