EN 10149-2 S700MC steel plate/sheet for High yield strength cold forming steel

Key words: S700MC steel plate/sheet, EN 10149-2 S700MC steel plate/sheet, S700MC steel plate/sheet supplier/Chinese supplier, S700MC steel plate/sheet price, S700MC steel plate/sheet mechanical property.

EN 10149-2 S700MC steel equivalent grade:
S700MC steel plate/sheet is in EN 10149-2 standard, the material number is 1.8969. The equivalent grades of S700MC steel are SEW092 QStE 690TM, NFA36-231 E690D, ASTM A514, BS1449 75F70.

| S700MC EN 10149-2 Number:1.8974 | Comparision of steel grades |
| --- | --- |
|  | SEW092 | QStE 690TM |
|  | NFA36-231 | E690D |
|  | ASTM | A514 |
|  | BS1449 | 75F70 |

EN 10149-2 S700MC steel chemical composition %:
Main chemical composition in EN 10149-2 S700MC steel is carton max 0.12, silicon max 0.60, manganese max 2.1, phosphorus max 0.025, Sulphur max 0.015. More detailed information about S700MC steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | AL max | Nb max | V max | Ti max | Mo max | B max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S700MC | 0.12 | 0.6 | 2.1 | 0.025 | 0.015 | 0.015 | 0.09 | 0.2 | 0.22 | 0.5 | 0.005 |

EN 10149-2 S700MC steel mechanical property:

| Nominal thickness(mm) | - |
| --- | --- |
| ReH-Minimun yield strength(Mpa) | 700 |

| Nominal thickness(mm) | - |
| --- | --- |
| Rm-Tensile strength(Mpa) | 750-950 |

| Nominal thickness(mm) | From3 |
| --- | --- |
| A-Minimum elongation Lo=5,65√So(%) | 12 |

| Nominal thickness(mm) | to3 |
| --- | --- |
| A-Minimum elongation Lo=Lo=80mm(%) | 10 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10149-2 S700MC steel are available, so if need, welcome to contact ICE steel sales team.