EN10025 E 335 steel plate/sheet for general Construction steels
Key words :
EN10025 E 335 steel plate/sheet,EN10025 E 335 steel plate/sheet, under EN standard, we can regard E 335 steel plate/sheet for general Construction steels.EN10025 E 335 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of EN E 335 steel.E 335 steel is according to EN10025 standard and it is equivalent to EN:Fe690-2,DIN17100:St70-2,NFA: A70-2 and UNI7070:Fe690 steel grades.
Equivalent grade : 
EN10025 E 335  steel plate/sheet is in EN10025 standard. The comparison of steel grades is: EN10025:1990 E 335，DIN17100 ST60-2, NFA 35-501 A60-2,BS1449,UNI7070 FE 590.

| E 335 EN 10025(93) Number: 1.0060 | Comparison of steel grades |
| --- | --- |
|  | EN 10025(90) | Fe 590-2 |
|  | NBNA21201 | A 590-1,2 |
|  | DIN 17100 | St 60-2 |
|  | NFA 35501 | A 60-2 - |
|  | MNC 850 E | SIS 16,50,00 |
|  | ISO 1052 | Fe E 590 |
|  | UNI 7070 | Fe 590 |
|  | JISG |  |

E 335 steel Chemical analysis
Main chemical composition in EN10025 E 335  steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| E335 | - | - | - | - | 0.045 | 0.045 | 0.012 |

E 335 steel Mechanical properties 
EN10025 E 335 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about EN10025 E 335 steel Mechanical Properties , please refer to the following table:

Mechanical properties

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 335 325 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 590-770 570-710 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 7 8 9 10 14 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.