EN10025 S235J0 carbon steel

Key words :
S235J0 steel plate, under EN10025(93) standard S235J0 steel plate, under EN10025(93) standard, we can regard S235J0 steel plate as Carbon steel
S235J0 steel plate is one mainly of Carbon steel, S235J0 steel plate is a structural steel grade which be used in riveted, bolted, or welded construction of bridges and buildings.It is identical to DIN:St37-3U,BS:40C,JIS:SM400B and Fe360C and etc 
Equivalent grade : 
S235J0 steel plate/sheet is in EN10025 standard. It's grade Number is 1.0114. The equal material of S235J0 is: EN10025:1990 FE 360 C, DIN17100 ST37-3U, NFA 35-501 E24-3, JIS3101 SS400B,UNI7070 FE 360 C .

| S235J0 DIN EN 10025-2Number: 1.0114 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE E 360 C |
|  | DIN17100 | ST37-3U |
|  | NFA 35-501 | E24-3 |
|  | BS1449 | 40C |
|  | JIS3106 | SM400B |
|  | UNI7070 | FE 360 C |

EN10025 S235J0 steel Chemical Composition % : 
 
Main chemical composition in EN10025 S235j0 steel : Manganese max 1.4, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

EN10025 S235J0 steel Mechanical Properties

EN10025 S235J0 steel plate/sheet for carbon steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S235J0 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t ≤ 16mm t >16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S235J0 sheet, S235J0 Cross Reference, S235J0 Schematic, S235j0 Distributor, S235j0 Equivalent, S235j0 Application Note, S235j0 Data Sheet, S235j0 component, S235j0 Fiche Technique, S235j0 Circuit, S235j0 steel sheet, S235j0 steel price. S235j0 steel supplier, S235j0 steel manufacturer.