EN10025 S235JR carbon steels

Key words : 
S235JR steel plate, under EN10025 standard S235JR steel plate, under EN10025 standard, we can regard S235JR steel plate as Carbon steel

S235JR steel plate is one mainly of Carbon steel, S235JR steel plate is a type of steel sheet under EN standard which is used to build ship, bridge, belongs to high strength sheet. S235JR is equivalent to DIN:St37-2,JIS:SS400,ASTM:A283C and UNI:FE360B
Equivalent grade : 
S235JR steel plate/sheet is in EN10025 standard. It's grade Number is 1.0037. The equal material of S235JR is: EN10025:1990 FE 360 B, DIN17100 ST37-2, NFA 35-501 E24-2, JIS3101 SS400 - ASTM A283C,UNI7070 FE 360 B .

| S235JR DIN EN 10025-2Number: 1.0037 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 360 B |
|  | DIN17100 | ST37-2 |
|  | NFA 35-501 | E24-2 |
|  | JIS3101 | SS400 |
|  | ASTM | A283C |
|  | UNI7070 | FE 360 B |

EN10025 S235JR steelChemical Composition % : 
 
Main chemical composition in EN10025 S235JR steel : Manganese max 1.4, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.20 | -- | 1.40 | 0.045 | 0.045 |

EN10025 S235JR steel Mechanical Properties

EN10025 S235JR steel plate/sheet for carbon steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S235JR steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm [N/mm2]transv. | Fracture Elongation[%] transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 235 225 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥3mm |  |  | 16 17 18 19 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S235JR sheet, S235JR Cross Reference, S235JR Schematic, S235JR Distributor, S235JR Equivalent, S235JR Application Note, S235JR Data Sheet, S235JR component, S235JR Fiche Technique, S235JR Circuit, S235JR steel sheet, S235JR steel price. S235JR steel supplier, S235JR steel manufacturer.