EN10025 S275J0 low alloy steel

Key words :
S275J0 steel plate, under EN10025(93) standard S275J0 steel plate, under EN10025(93) standard, we can regard S275J0 steel plate as low alloy steel
S275J0 steel plate is one mainly of low alloy steel, S275J0 alloy steel plate is equal to DIN:St44-3U,NFA:E28-3,BS:43C and UNI:Fe430C.The tensile strength of S275Jo is 430-580MPa when its thickness is less than 3mm

Equivalent grade : 
S275J0 steel plate/sheet is in EN10025 standard. It's grade Number is 1.0044. The equal material of S275J0 is: EN10025:1990 FE 430 C, DIN17100 ST44-3U, NFA 35-501 E28-3, BS1449 43C UNI7070 FE 430 C .

| S275J0 DIN EN 10025-2Number: 1.0143 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 430 C |
|  | DIN17100 | ST44-3U |
|  | NFA 35-501 | E28-3 |
|  | BS1449 | 43C |
|  | UNI7070 | FE 430 C |

EN10025 S275J0 steel Chemical Composition % : 
 
Main chemical composition in EN10025 S275J0 steel : Manganese max 1.5, Phosphorus max 0.040,Sulphur max 0.040. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.18 | -- | 1.50 | 0.040 | 0.040 |

EN10025 S275J0 steel Mechanical Properties

EN10025 S275J0 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S275J0 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%] transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | 0 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S275J0 sheet, S275J0 Cross Reference, S275J0 Schematic, S275J0 Distributor, S275J0 Equivalent, S275J0 Application Note, S275J0 Data Sheet, S275J0 component, S275J0 Fiche Technique, S275J0 Circuit, S275J0 steel sheet, S275J0 steel price. S275J0 steel supplier, S275J0 steel manufacturer.