EN10025 S275J2 low alloy steel

Key words : 
S275J2 steel plate, under EN10025(93) standard S275J2 steel plate, under EN10025(93) standard, we can regard S275J2 steel plate as low alloy steel
S275J2 steel plate is one mainly of low alloy steel, S275j2 steel is a structural steel grade which be used in riveted, bolted, or welded construction of bridges and building.

EN10025 S275J2 steel Chemical Composition
 
Main chemical composition in EN10025 S275J2 steel : Manganese 1.6, Phosphorus 0.035,Sulphur max 0.035. More detailed information, please refer to the flowing table:

| Grade | C % | Si % | Mn % | P % | S % | N % | Cu % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S275J2 | 0.210 | - | 1.600 | 0.035 | 0.035 | - | 0.060 |

EN10025 S275J2 steel Mechanical Properties 
EN10025 S275J2 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity, processing property. More detailed information about EN10025 S275J2 steel Mechanical Properties , please refer to the following table:

| Grade | Thickness(mm) | Min Yield (Mpa) | Tensile(MPa) | Elongation(%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| S275j2 | 8mm-100mm | 275Mpa | 430-560Mpa | 21-23% | -20 | 27J |
|  | 101mm-200mm | 225-235Mpa | 400-540Mpa | 19% | -20 | 27J |
|  | 201mm-400mm | 215Mpa | 380-540Mpa | 18% | -20 | 27J |
| The min impact energy is longitudinal energy |

ICE steel is the professional Chinese steel exporter. We can offer you S275J2 sheet, S275J2 Cross Reference, S275J2 Schematic, S275J2 Distributor, S275J2 Equivalent, S275J2 Application Note, S275J2 Data Sheet, S275J2 component, S275J2 Fiche Technique, S275J2 Circuit, S275J2 steel sheet, S275J2 steel price. S275J2 steel supplier, S275J2 steel manufacturer.