EN10025 S275N low alloy steel
Key words : 
S275N steel plate, under EN10113-2 standard S275N steel plate, under EN10113-2 standard, we can regard S275N steel plate as low alloy steel
S275N steel plate is one mainly of low alloy steel,S275N steel plate is under EN10025-3 standard equivalent to DIN:StE285,which with a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of S275N is 370 to 510MPa 
Equivalent grade : 
S275N steel plate/sheet is in EN10025 standard. It's grade Number is 1.0490. The equal material of S275N is: UNE36081: AE285KG/AE285KW, DIN17102 STE285, NFA 36-207, UN Fe E 275KG N.

| S275N EN 10025-3 MATERIAL# 1.0490 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE285KG/AE285KW |
|  | DIN17102 | STE285 |
|  | NFA 36-207 | - |
|  | UN | Fe E 275KG N |

EN10025 S275N steel Chemical Composition % : 
 
Main chemical composition in EN10025 S275N steel : Manganese 0.50-1.50, Phosphorus max 0.030,Sulphur max 0.025. More detailed information, please refer to the flowing table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.40 | 0.50-1.50 | 0.030 | 0.025 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

EN10025 S275N steel Mechanical Properties

EN10025 S275N steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S275N steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S275N sheet, S275N Cross Reference, S275N Schematic, S275N Distributor, S275N Equivalent, S275N Application Note, S275N Data Sheet, S275N component, S275N Fiche Technique, S275N Circuit, S275N steel sheet, S275N steel price. S275N steel supplier, S275N steel manufacturer