EN10025 S275NL low alloy steel
Key words : 
S275NL steel plate, under EN10113-2 standard S275NL steel plate, under EN10113-2 standard, we can regard S275NL steel plate as low alloy steel
S275NL steel plate is one mainly of low alloy steel, S275NL steel plate is a hot rolled structural steels, which technical delivery conditions for normalized or normalized rolled in weldable fine grain structural steel grade. It is also regarded as DIN:TStE285 and BS:43EE 
Equivalent grade : 
S275NL steel plate/sheet is in EN10025 standard. It's grade Number is 1.0044. The equal material of S275NL is: UNE36081 AE 285 KT, DIN17102 T StE 285, UN Fe E 275 KT N,BS4360 43 EE ,

| S275NL EN 10025-3 MATERIAL# 1.0491 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 285 KT |
|  | DIN17102 | T StE 285 |
|  | UN | Fe E 275 KT N |
|  | BS4360 | 43 EE |

EN10025 S275NL steel Chemical Composition% : 
 
Main chemical composition in EN10025 S275NL steel : Manganese 0.50-1.50, Phosphorus max 0.025,Sulphur max 0.020. More detailed information, please refer to the flowing table:

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.16 | 0.40 | 0.50-1.50 | 0.025 | 0.020 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

EN10025 S275NL steel Mechanical Properties

EN10025 S275NL steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S275NL steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S275NL sheet, S275NL Cross Reference, S275NL Schematic, S275NL Distributor, S275NL Equivalent, S275NL Application Note, S275NL Data Sheet, S275NL component, S275NL Fiche Technique, S275NL Circuit, S275NL steel sheet, S275NL steel price. S275NL steel supplier, S275NL steel manufacturer