EN10025 S355J0 low alloy steel

Key words : 
S355J0 steel plate, EN10025 S355J0 steel plate, under EN10025 standard, we can regard S355J0 steel plate as low alloy steel
S355J0 steel plate is one mainly of low alloy steel, S355J0 steel plate S355J0 Material number 1.0553 According to EN10025 1. In different standards, we can regard S355J0 steel plate as different name. the detail information is as follows DIN 17100： St 52-3 U NFA 35-501： E 36-3 UNI 7070：Fe 510 C 
Equivalent grade : 
S355J0 steel plate/sheet is in EN10025 standard. It's grade Number is 1.0553. The equal material of S355J0 is: EN10025:1990 FE 510 C, DIN17100 ST52-3U, NFA 35-501 E36-3, BS1449 50C - UNI7070 A283C.

| S355J0 DIN EN 10025-2 Number: 1.0553 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 C |
|  | DIN17100 | ST52-3U |
|  | NFA 35-501 | E36-3 |
|  | BS1449 | 50C |
|  | UNI7070 | FE 510 C |

EN10025 S355J0 steel Chemical Composition % : 
 
Main chemical composition in EN10025 S355J0 steel : Manganese max 1.6, Phosphorus max 0.040,Sulphur max 0.040. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.20 | 0.55 | 1.60 | 0.040 | 0.040 |

EN10025 S355J0 steel Mechanical Properties

EN10025 S355J0 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S355J0 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 0 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S355J0 sheet, S355J0 Cross Reference, S355J0 Schematic, S355J0 Distributor, S355J0 Equivalent, S355J0 Application Note, S355J0 Data Sheet, S355J0 component, S355J0 Fiche Technique, S355J0 Circuit, S355J0 steel sheet, S355J0 steel price. S355J0 steel supplier, S355J0 steel manufacturer.