EN10025 S355J2 low alloy steel

Key words : 
S355J2 steel plate, EN10025 standard S355J2 steel plate, under EN10025 standard, we can regard S355J2 steel plate as low alloy steel
S355J2 steel plate is one mainly of low alloy steel, S355J2 steel plate S355J2G3 is a high tensile low carbon structural steel with minimum yield strength of S355N/mm2, this structural and shipbuilding steels are according to material standards and project-specific requirement. This structural steels can be delivered in either normalized, mormalized + boron or thermomechanically rolled condition, this steel grade benefits to high strength structures, on the other hand weight saving in the final structure due to plate thickness can be reduced, thus increased effective loads during use as well as cost saving in fabrication

EN10025 S355J2 steel Chemical Composition
Main chemical composition in EN10025 S355J2 steel : Carbon max 0.23-0.24,Silicium max 0.60,Manganese max 1.7, Phosphorus max 0.035,Sulphur max 0.035. More detailed information, please refer to the flowing table:

| Grade | C % | Si % | Mn % | P % | S % | N % | Cu % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S355J2 | 0.23-0.24 | 0.600 | 1.700 | 0.035 | 0.035 | … | 0.060 |

EN10025 S355J2 steel Mechanical Properties

EN10025 S355J2 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S355J2 steel Mechanical Properties , please refer to the following table:

| Grade | Thickness(mm) | Min Yield (Mpa) | Tensile(MPa) | Elongation(%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| S355J2 | 8mm-100mm | 315Map-355Mpa | 450-630Mpa | 18-20% | -20 | 27J |
|  | 101mm-200mm | 285Mpa-295Mpa | 450-600Mpa | 18% | -20 | 27J |
|  | 201mm-400mm | 275Mpa | 450-600Mpa | 17% | -20 | 27J |
| The min impact energy is longitudinal energy |

ICE steel is the professional Chinese steel exporter. We can offer you S355J2 sheet, S355J2 Cross Reference, S355J2 Schematic, S355J2 Distributor, S355J2 Equivalent, S355J2 Application Note, S355J2 Data Sheet, S355J2 component, S355J2 Fiche Technique, S355J2 Circuit, S355J2 steel sheet, S355J2 steel price. S355J2 steel supplier, S355J2 steel manufacturer.