EN10025 S355JR low alloy steel 
Key words : 
S355JR steel plate, under EN10025(93) standard S355JR steel plate, under EN10025(93) standard, we can regard S355JR steel plate as low alloy steel
S355JR steel plate is one mainly of low alloy steel, S355JR steel plate is alloy steel under the EN standard which is equal to DIN17100:St52-3,JIS:SS490/SM490A,BS:50B and UNI7070:Fe510B 
Equivalent grade : 
S355JR steel plate/sheet is in EN10025 standard. It's grade Number is 1.0045.The equal material of S355JR is: EN10025:1990 FE 510 B, DIN17100 ST52-3, NFA 35-501 E36-2, JIS SS490/SM490A - ASTM A572GR50,UNI7070 FE 510 B .

| S355JR EN 10025-2Number: 1.0045 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | ASTM | A572GR50 |
|  | JIS | SS490/SM490A |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

EN10025 S355JR steel Chemical Composition
 
Main chemical composition in EN10025 S355JR steel : Silicium max 0.55 Manganese max 1.60, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

EN10025 S355JR steel Mechanical Properties

EN10025 S355JR steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S355JR steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | Tensile StrengthRm[N/mm2]transv. | Fracture Elongation [%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S355JR sheet, S355JR Cross Reference, S355JR Schematic, S355JR Distributor, S355JR Equivalent, S355JR Application Note, S355JR Data Sheet, S355JR component, S355JR Fiche Technique, S355JR Circuit, S355JR steel sheet, S355JR steel price. S355JR steel supplier, S355JR steel manufacturer.