EN10025 S355N steel plate low alloy steel

Key words : 
S355N steel plate, under EN10113-2 standard S355N steel plate, under EN10113-2 standard, we can regard S355N steel plate as low alloy steel
S355N steel plate is one mainly of low alloy steel, S355N steel plate under EN10025-3 standard, it is normalized , fine grain structural steel which is regarded as other standards,like:DIN-StE355,NFA-E355R and UN-FeE355KGN 
Equivalent grade : 
S355N steel plate/sheet is in EN10025 standard. It's grade Number is 1.0545. The equal material of S355N is: UNE36081 AE355KG/AE355KW , DIN17102 STE355, NFA 36-201 E355R, BS4036 ,UN Fe E 3555KG N .

| S355N EN 10025-3 MATERIAL#1.0545 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE355KG/AE355KW |
|  | DIN17102 | STE355 |
|  | NFA 36-201 | E355R |
|  | BS4036 | - |
|  | UN | Fe E 3555KG N |

EN10025 S355N steel Chemical Composition
 
Main chemical composition in EN10025 S355N steel : Carbon max 0.20,Silicium max 0.50, Manganese max 0.90-1.65, Phosphorus max 0.030,Sulphur max 0.025. More detailed information, please refer to the flowing table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.50 | 0.90-1.65 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

EN10025 S355N steel Mechanical Properties

EN10025 S355N steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about EN10025 S355N steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |

ICE steel is the professional Chinese steel exporter. We can offer you S355N sheet, S355N Cross Reference, S355N Schematic, S355N Distributor, S355N Equivalent, S355N Application Note, S355N Data Sheet, S355N component, S355N Fiche Technique, S355N Circuit, S355N steel sheet, S355N steel price. S355N steel supplier, S355N steel manufacturer.