EN10028 16Mo3 steel plate/sheet for boiler steels

Key words :
16Mo3 steel plate/sheet, EN10028 16Mo3 steel plate/sheet, EN10028 16Mo3 steel plate/sheet for boiler steel, 16Mo3 carbon steel used for boiler, EN10028 steel plate for boiler using, 16Mo3 steel supplier/Chinese supplier, 16Mo3 steel price...

Equivalent grade : 
16Mo3 steel plate/sheet is in EN10028-2 standard. It's grade Number is 1.5415. The equal material of 16Mo3 is: DIN 17155 15Mo3, NFA 36-205 15 D3, UNI 5869 15Mo3, BS 1501 1503 - 243 B, UNE 36087 16Mo3, ASTM A 204 Gr. B.

| 16Mo3 EN 10028-2 Number:1.5415 | DIN 17155 | 15 Mo 3 |
| --- | --- | --- |
|  | NFA 36-205 | 15 D3 |
|  | UNI 5869 | 15 Mo 3 |
|  | BS 1501 | 1503 - 243 B |
|  | UNE 36087 | 16 Mo 3 |
|  | ASTM | A 204 Gr. B |

EN10028-2 16Mo3 steel Chemical Composition % :

Main chemical composition in EN10028-2 16Mo3 steel : Carbon: from 0.12 to 0.2 , Manganese from 0.40 to 0.90, Sulphur max 0.01, Phosphorus max 0.025, Silicon max 0.35, Molybdenum from 0.25 to 0.35, Chromium max 0.30. More detailed information, please refer to the flowing table:

| Grade | C. max | Mn. | S. | N | Cu | Si. | P. | Cr. | Ni. | Mo. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 16Mo3 | 0.12- 0.2 | 0.40- 0.90 | 0.01 | 0.012 | 0.30 | 0.35 | 0.025 | 0.30 | 0.30 | 0.25- 0.35 |

EN10028-2 16Mo3 steel Mechanical Properties

16Mo3 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 220-275 MPa (there is different min strength point at the different thickness.) 16Mo3 tensile strength is from 440MPa to 590MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 16Mo3 steel Mechanical Properties , please refer to the following table:

| Grade | Tensile Strength (Mpa) | Yield Strength (Mpa) | Elongation in 100-150 mm(%) | Elongation in 16 mm(%) | Max Thickness (mm) |
| --- | --- | --- | --- | --- | --- |
| 16Mo3 | 440-590 | 220-275 | 19 | 24 | 250 |