EN10111 DD11 steel plate/sheetfor stamping and cold forming steels
EN10111 DD11 steel plate/sheet,DD11 steel plate/sheet, under EN standard, EN10111 DD11 steel plate/sheet for stamping and cold forming steels,DD11 steel supplier/Chinese supplier, DD11 steel price,DD11 steel manufacturer.

DD11 steel plate/sheet is in EN10111 standard. It's grade Number is 1.0332. The equal material of DD11 is: DIN 1614 STW22, NFA 36-301 1C, UNI5867 FEP11, BS1449 HR3,UNE36.093  AP11, ASTM-SAE A621DQ-SAE1010,JIS G 3131 SPHD.

| DD11 EN 10111 Number: 1.0332 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | FEP11 |
|  | DIN1614 | STW22 |
|  | NFA 36-301 | 1C |
|  | JIS G 3131 | SPHD |
|  | ASTM-SAE | A621DQ-SAE1010 |
|  | BS1449 | HR3 |
|  | UNE36.093 | AP11 |

Main chemical composition in EN10111 DD11 steel: Carbon:max 0.12, Manganese max 0.60, Sulphur max 0.045, Phosphorus max 0.045. More detailed information, please refer to the flowing table: 
DD11 steel Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| DD11 | 0.12 | -- | 0.60 | 0.045 | 0.045 |

EN10111 DD11 steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.It's tensile strength is around 440 MPa (there is different min strength point at the different thickness.) DD11 yield strength is from 170MPa to 340 MPa. (different min strength point at the different thickness.) More detailed information about EN10111 DD11 steel Mechanical Properties , please refer to the following table:
Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-340 |  |  | 1 S |
| t < 3mm t ≥ 3mm |  | 440 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 23 A80 24 A80 28 A5 |  |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN10111 DD11 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products EN10111 DD11 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.