EN10111 DD12 steel plate/sheet for stamping and cold forming steels
EN10111 DD12 steel plate/sheet,DD12 steel plate/sheet, under EN standard, EN10111 DD12 steel plate/sheet for stamping and cold forming steels,DD12 steel supplier/Chinese supplier, DD12 steel price,DD12 steel manufacturer.

DD12 steel plate/sheet is in EN10111 standard. It's grade Number is 1.0398. The equal material of DD12 is: DIN 1614 RRSTW23,ASTM-SAE A621DQ-SAE1008,JIS G 3131 SPHE.

| DD12 EN 10111 Number: 1.0398 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | - |
|  | DIN1614 | RRSTW23 |
|  | NFA 36-301 | - |
|  | JIS G 3131 | SPHE |
|  | ASTM-SAE | A621DQ-SAE1008 |
|  | UNE36.093 | - |

Main chemical composition in EN10111 DD12 steel: Carbon max 0.10, Manganese max 0.45,Phosphorus max 0.035, Sulphur max 0.035,More detailed information,please refer to the flowing table: 
DD12 steel Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| DD12 | 0.10 | -- | 0.45 | 0.035 | 0.035 |

EN10111 DD12 steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.It's yield strength is between 170 to 320 MPa (there is different min strength point at the different thickness.) DD12 tensile strength is from around 420 MPa. (different min strength point at the different thickness.) More detailed information about EN10111 DD12 steel Mechanical Properties , please refer to the following table: 
Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-320 |  |  | 0 S |
| t < 3mm t ≥ 3mm |  | 420 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 25 A80 26 A80 30 A5 |  |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN10111 DD12 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products EN10111 DD12 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.