EN10111 DD13 steel plate/sheet for stamping and cold forming steels
EN10111 DD13 steel plate/sheet,DD13 steel plate/sheet, under EN standard, EN10111 DD13 steel plate/sheet for stamping and cold forming steels,DD13 steel supplier/Chinese supplier, DD13 steel price,DD13 steel manufacturer.

DD13 steel plate/sheet is in EN10111 standard. It's grade Number is 1.0335. The equal material of DD13 is:NFA 36-301 3C, UNI5867 FEP13, BS1449 HR1,UNE36.093  AP13, ASTM-SAE A621DQ-SAE1006AK,JIS G 3131 SPHE AK.

| DD13 EN 10111 Number: 1.0335 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | FEP13 |
|  | BS1449 | HR1 |
|  | NFA 36-301 | 3C |
|  | JIS G 3131 | SPHE AK |
|  | ASTM-SAE | A621DQ-SAE1006AK |
|  | UNE36.093 | AP13 |

Main chemical composition in EN10111 DD13 steel: Carbon:max 0.08, Manganese max 0.40, Sulphur max 0.030, Phosphorus max 0.030. More detailed information, please refer to the flowing table: 
Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| DD13 | 0.08 | -- | 0.40 | 0.030 | 0.030 |

EN10111 DD13 steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.It's yield strength is between 170 to 310 MPa (there is different min strength point at the different thickness.) DD13 tensile strength is around 400 MPa. (different min strength point at the different thickness.) More detailed information about EN10111 DD13 steel Mechanical Properties , please refer to the following table:
Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-310 |  |  | 0 S |
| t < 3mm t ≥ 3mm |  | 400 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 28 A80 29 A80 33 A5 |  |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN10111 DD13 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products EN10111 DD13 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.