EN10111 S355NL steel plate/sheetfor fine-grain structural steel

Key words: S355NL steel plate/sheet, EN 10111 S355NL steel plate/sheet, S355NL steel plate/sheet supplier/Chinese supplier, S355NL steel plate/sheet price, S355NL steel plate/sheet mechanical property.

EN 10111 S355NL steel Equivalent grade: 
S355NL steel plate/sheet is in EN 10111 standard, the grade number is 1.0546. The equivalent materials of S355NL steel are UNE36081 AE 355 KT, DIN17102 T StE 355, UN Fe E 355 KT N, NFA36 201 E355FP, BS1449 50 EE.

| S355NL EN 10111 MATERIAL# 1.0546 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 355 KT |
|  | DIN17102 | T StE 355 |
|  | UN | Fe E 355 KT N |
|  | NFA36 201 | E355FP |
|  | BS1449 | 50 EE |

EN 10111 S355NL steel chemical composition %:

Main chemical composition of EN 10111 S355NL steel is carton max 0.18, silicon max 0.50, manganese from 0.90-1.65, phosphorus max 0.025, Sulphur max 0.020, chromium max 0.30. More detailed information about S355NL steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.50 | 0.90-1.65 | 0.025 | 0.020 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

EN 10111 S355NL steel mechanical property:
S355NL steel plate is one mainly of Fine-grain structural steels, normalised rolled, The normalized rolled fine-grain structural steel S355NL is characterized by a minimum yield strength of 355 MPa, by good weldability and high resistance to brittle fracture. More detailed information about S355NL steel, please refer to the down table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10111 S355NL steel are available, so if need, welcome to contact ICE steel sales team.