JIS 3101 SS 540 steel plate/sheet for High Yield Steel
Key words: SS 540 steel plate/sheet, JIS 3101 SS 540 steel plate/sheet, SS 540 steel plate/sheet supplier, SS 540 steel plate/sheet mechanical property, SS 540 steel plate/sheet price.

JIS 3101 SS 540 steelequivalent grade:
SS 540 steel plate/sheet is in JIS 3101 standard, the equivalent grade are DIN 17102 STE 380, NFA 36201 E 375R, MNC 810E SS21,42,01, CSA G40-21 400 W, WT, ASTM A 572gr. 60,65.

| SS 540 JIS 3101 | Comparision of steel grades |
| --- | --- |
|  | DIN 17102 | STE 380 |
|  | NFA 36201 | E 375R |
|  | MNC 810E | SS21,42,01 |
|  | CSA G40-21 | 400 W, WT |
|  | ASTM | A 572gr. 60,65 |

JIS 3101 SS 540 steel chemical composition %:
Main chemical composition in JIS 3101 SS 540 steel is carton max 0.26, silicon max 0.40, manganese max 1.35, phosphorus max 0.04, Sulphur max 0.05. More detailed information about SS 540 steel, please refer to the down table:

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| Grade60 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |
| Grade65 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |

JIS 3101 SS 540 steel mechanical property:
JIS 3101 SS 540is high strength low alloy steel plate sheet which is widely used in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles, excavators, loaders, bulldozers , various types of cranes, hydraulic support, coal mining machinery and equipments and other structures.

| Symbol | Yield point min MPa | Tensile strength MPa | Elongation in 2 in.(50mm)% |
| --- | --- | --- | --- |
| Grade A | 165 | 310-450 | 30 min |
| Grade B | 185 | 345-450 | 28 min |
| Grade C | 205 | 380-515 | 25 min |
| Grade D | 230 | 415-550 | 23 min |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of JIS 3101 SS 540 steel are available, so if need, welcome to contact ICE steel sales team.