JIS G 3116 SG255 steel plate/sheet for gas cylinders and gas vessels

Key words :
SG255 steel plate/sheet, JIS G 3116 SG255 steel plate/sheet, JIS G 3116 SG255 steel plate/sheet for gas cylinder and gas vessel, SG255 carbon steel used for gas cylinder and gas vessel, JIS G 3116 steel plate for gas cylinder and gas vessel, SG255 steel supplier/Chinese supplier, SG255 steel price...

Equivalent grade : 
SG255 steel plate/sheet is in JIS G 3116 standard. It's grade Number is 1.0111. The equal material of SG255 is: EN10120 P245NB, DIN17155 HI, NFA 36-211 BS1 ,UNI 7355 FE E24KR, BS 5045 - TYPE A, UNE 36129 AE235KR.

| SG255 JIS G 3116 Number:1.0111 | EN10120 | P245N |
| --- | --- | --- |
|  | DIN17155 HI | HI |
|  | NFA 36-211 | BS1 |
|  | UNI 7355 | FE E24KR, |
|  | BS 5045 | TYPE A |
|  | UNE 36129 | AE235KR |

JIS G3116 SG255  steel Chemical Composition %

Main chemical composition in JIS G 3116 SG255 steel : Carbon: max 0.20 , Manganese max 0.30 , Sulphur max 0.04, Phosphorus max 0.040, More detailed information, please refer to the flowing table:

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| SG255 | 0.20 | - | 0.30 | 0.040 | 0.040 |

JIS G3116 SG255 steel Mechanical Properties

SG255 this material is mainly used to fabricate gas cylinder and gas vessel. this kind of steel has the good grain and Mechanical properties. It's yield strength is min 255 MPa (there is different min strength point at the different thickness.) SG255 tensile strength is min 440MPa .(different min strength point at the different thickness.) More detailed information about JIS G3116 SG255  steel Mechanical Properties , please refer to the following table:

| Symbol | Yield point or proof stress N/mm2 (min) | Tensile strength N/mm2 min | Elongation % min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Bending Angle | Inside radius | Test piece |
| SG255 | 255 | 400 | 26 | NO.5 in rolling direction | 180° | Thickness x 1.0 Thickness x 1.5 | No.3 in rolling direction |

ICE steel is the professional steel exporter in china, We devote extraordinary resources to listening to our customers—to understanding their individual and evolving needs, the characteristics of their markets, and the trends that influence them. Combining insights with innovation, we not only stay in step with our customers, but also keep miles ahead of the competition. we will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.