JIS G 4051 S35Csteel plate high carbon steel 
S35Csteel plate, JIS G 4051 S35Csteel plate, S 35 C high carbon steel plate and sheet, JIS G 4051 steel plate, S 35 C carbon steel supplier/Chinese S 35 C Steel supplier, S 35 C Steel price,S 35 C steel manufacturer.

S 35 C steel plate is one mainly of high carbon steel,the application of JIS G 4051 S 35 C steel plate is equal to DIN 1C35, AISI 1035.

The equivalent standards of S35C steel

| S35C JIS G 4051 | Comparison of steel grades |
| --- | --- |
|  | DIN | 1C35 |
|  | AISI | 1035 |
|  | UNI 7846 | - |
|  | BS 970 | - |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | - |

Main chemical composition in JIS G 4051 S 35 C steel : Carbon: from 0.32 to 0.38, Manganese from 0.60 to 0.90, Sulphur max 0.030, Phosphorus max 0.030, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of S 35 C steel

| Grade | C | Si | Mn | P(%) max | S(%) max | Cr(%) max | Ni(%) max | Cu(%) max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S35C | 0.32-0.38 | 0.15-0.35 | 0.60-0.90 | 0.030 | 0.030 | 0.20 | 0.20 | 0.30 |

S 35 C high carbon steel has the good grain and Mechanical properties. It's yield strength is between 310-440 MPa ,       S 35 C tensile strength is from 480MPa to 1690MPa. More detailed information about JIS G 4051 S 35 C steel Mechanical Properties , please refer to the following table:

Mechanical Properties of S 35 C steel

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C35 | Rolled Annealed Water-quenched Oil quenched | 440 310 | 700 480 1845 1690 | 18 30 | 53 50 | 840 880 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like JIS G 4051 S 35 C steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  JIS G 4051 S 35 C steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.