JIS G 4051 S 45 C steel plate high carbon steel 
S 45 C steel plate, JIS G 4051 S 45 C steel plate, S 45 C high carbon steel plate and sheet, JIS G 4051 steel plate, S 45 C carbon steel supplier/Chinese S 45 C steel supplier, S 45 C steel price,S 45 C steel manufacturer.

S45C steel plate is one mainly of high carbon steel,S45C is suitable for shafts studs, keys etc. Available as rolled or normalised. Supplied as square bar, or round bar or flat. They are excelling in weld ability & machine ability, and they can be subjected to various heat treatments which is based on JIS G 4051-2009.

| S45C JIS G 4051 | Comparison of steel grades |
| --- | --- |
|  | DIN | 1C45 |
|  | AISI | 1045 |
|  | UNI 7846 | - |
|  | BS 970 | - |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | - |

Main chemical composition in JIS G 4051 S 45 C steel : Carbon: from 0.42 to 0.50, Manganese from 0.50 to 0.80, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of S 45 C steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| S 45 C | 0.42-0.50 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

S 45 C high carbon steel has the good grain and Mechanical properties. It's yield strength is between 330-460 MPa ,S 45 C tensile strength is from 540MPa to 2270MPa. More detailed information about JIS G 4051 S 45 C steel Mechanical Properties , please refer to the following table:

Mechanical Properties of S 45 C steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| S 45 C | Rolled Annealed Water-quenched Oil quenched | 460 330 | 750 540 2270 1980 | 18 30 | 58 55 | 820 860 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like JIS G 4051 S 45 C steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  JIS G 4051 S 45 C steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services