JIS G 4051 S55C steel plate high carbon steel 
S 55 C steel plate, JIS G 4051 S55C steel plate, S 55 C high carbon steel plate and sheet, JIS G 4051 steel plate, S 55 C carbon steel supplier/Chinese S 55 C steel supplier, S 55 C steel price,S 55 C steel manufacturer.

S55C steel plate is one mainly of high carbon steel,is treated high technical heat treatment and it helps you make Die Plate & Plastics Die Plate much easier with good quality.It is equal to EN C55,DIN17200 C55,BS970 070M55,SAE 1055 and so on.

| S55C JIS G 4051 Number:1.0535 | Comparison of steel grades |
| --- | --- |
|  | EN 10083-2 | C 55 |
|  | DIN 17200 | C 55 |
|  | NFA 33-101 | AF70-C 55 |
|  | UNI 7846 | C 55 |
|  | BS 970 | 070 M 55 |
|  | UNE 36011 | C 55 k |
|  | SAE J 403-AISI | 1055 |

Main chemical composition in JIS G 4051 S 55 C steel : Carbon: from 0.52 to 0.60, Manganese from 0.60 to 0.90, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of S 55 C steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| S 55 C | 0.52-0.60 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

S 55 C high carbon steel has the good grain and Mechanical properties. It's yield strength is between 350-500 MPa ,S 55 C tensile strength is from550MPa to 2510 MPa. More detailed information about JIS G 4051 S 55 C steel Mechanical Properties , please refer to the following table:

Mechanical Properties of S 55 C steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| S 55 C | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.recommended Bending radius (≤90°) | 3.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like JIS G 4051 S 55 C steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  JIS G 4051 S 55 C steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.