JIS G3101 SS 400 steel plate/sheetfor High Yield Steel

Key words: SS 400 steel plate/sheet, JIS G3101 SS 400 steel plate/sheet, SS 400 steel plate/sheet supplier/Chinese supplier, SS 400 steel plate/sheet mechanical property, SS 400 steel plate/sheet price.

JIS G3101 SS 400 steel equivalent grade:
SS 400 steel plate/sheet is in JIS G3101 standard, the material number is 1.0044. The equivalent grade of SS 400 steel are EN 10025 S275JR, DIN 17100 St 44-2, NFA 35-501 E 28-2, UNI 7070 Fe 430 B, BS 4360 43 B, UNE 36.080 AE 275 B, ASTM A 283 D - A 36.

| SS 400 JIS G3101 Material #: 1.0044 | Comparison of steel grades |
| --- | --- |
|  | EN 10025 | S275JR |
|  | DIN 17100 | St 44-2 |
|  | NFA 35-501 | E 28-2 |
|  | UNI 7070 | Fe 430 B |
|  | BS 4360 | 43 B |
|  | UNE 36.080 | AE 275 B |
|  | ASTM | A 283 D - A 36 |

JIS G3101 SS 400 steel chemical composition %:
Main chemical composition in EN 10028-3 P 460 NL1 steel is phosphorus max 0.05, Sulphur max 0.05. More detailed information about P 460 NL1 steel, please refer to the down table:

| Grade | Chemical Composition, % by weight |
| --- | --- |
|  | C. max | Si. max | Manganese | P. max | S. max |
| SS400 | - | - | - | 0.050 | 0.050 |

JIS G3101 SS 400 steel mechanical property:
JIS G3101 SS400 is a technical delivery conditions for general purpose structural steel.JIS G3101 SS400 is a type of steel sheet under JIS standard which is used to build ship, bridge, belongs to high strength sheet.

| Grade | Yield Strength min. (Mpa) | Tensile Strength MPa | Elongation min. % | Impact Resistance min.[J] |
| --- | --- | --- | --- | --- |
|  | Thickness ＜16 mm | Thickness ≥16mm |  | Thickness ＜5mm | Thickness 5-16mm | Thickness ≥16mm |  |
| SS400 | 245 | 235 | 400-510 | 21 | 17 | 21 | - |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of JIS G3101 SS 400 steel are available, so if need, welcome to contact ICE steel sales team.