JIS G3101 SS 490 steel plate/sheet for High Yield Steel

Key words: SS 490 steel plate/sheet, JIS G3101 SS 490 steel plate/sheet, SS 490 steel plate/sheet supplier/Chinese supplier, SS 400 steel plate/sheet mechanical property, SS 490 steel plate/sheet price.

JIS G3101 SS 490 steel equivalent grade:
SS 490 steel plate/sheet is in JIS G3101 standard, the material number is 1.0045. The equivalent grade of SS 490 steel are EN 10025 S355JR, NFA 35-501 E 36-2, UNI 7070 Fe 510 B, BS 4360 50 B, UNE 36.080 AE 355 B, ASTM A 572 Gr. 50 - A 678 Gr. A.

| SS 490 JIS G3101 Material #: 1.0045 | Comparison of steel grades |
| --- | --- |
|  | EN 10025 | S355JR |
|  | NFA 35-501 | E 36-2 |
|  | UNI 7070 | Fe 510 B |
|  | BS 4360 | 50 B |
|  | UNE 36.080 | AE 355 B |
|  | ASTM | A 572 Gr. 50 - A 678 Gr. A |

JIS G3101 SS 490 steel chemical composition %:
Main chemical composition in JIS G3101 SS 490 steel is carton max 0.24, silicon max 0.55, manganese max 1.60, phosphorus max 0.045, Sulphur max 0.045. More detailed information about JIS G3101 SS 490 steel, please refer to the down table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

JIS G3101 SS 490 steel mechanical property:
JIS G3101 SS490 is a technical delivery conditions for general purpose structural steel.JIS G3101 SS490 is a type of steel sheet under JIS standard which is used to build ship, bridge, belongs to high strength sheet.

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrength Rm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of JIS G3101 SS 490 steel are available, so if need, welcome to contact ICE steel sales team.