JIS G3101 SS400 carbon steel 
Key words :
JIS G3101 SS400 steel plate/sheet,JIS G3101 SS400 steel plate/sheet, under JISG3101 standard, we can regard SS400 steel plate/sheet for general purpose structural steel.
JIS G3101 SS400 is a technical delivery conditions for general purpose structural steel.JIS G3101 SS400 is a type of steel sheet under JIS standard which is used to build ship, bridge, belongs to high strength sheet. JIS G3101 SS400 is equivalent to DIN:St37-2,EN SS400,ASTM:A283C and UNI:FE360B.

Equivalent grade : 
SS400 steel plate/sheet is in JIS G3101 standard. The equal material of SS400 is: BS 4360 40(A)B, CSAG40-21 230 G, IS IS 226, JIS 3106 SM 400 A - ISO 630 Fe 360 B, ASTM A 36/A 283 C.

| SS400 JIS3101 | Comparision of steel grades |
| --- | --- |
|  | BS 4360 | 40(A)B |
|  | CSAG40-21 | 230 G |
|  | IS | IS 226 |
|  | JIS 3106 | SM 400 A |
|  | ISO 630 | Fe 360 B |
|  | ASTM | A 36/A 283 C |

JIS G3101 SS400 steel Chemical Composition 
 
Main chemical composition in JIS G3101 SS400 steel : Phosphorus max 0.050,Sulphur max 0.050. More detailed information, please refer to the flowing table:

| Grade | Chemical Composition, % by weight |
| --- | --- |
|  | C. max | Si. max | Manganese | P. max | S. max |
| SS400 | - | - | - | 0.050 | 0.050 |

JIS G3101 SS400 steel Mechanical Properties

JIS G3101 SS400 steel plate/sheet for carbon steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about JIS G3101 SS400 steel Mechanical Properties , please refer to the following table:

| Grade | Yield Strength min. (Mpa) | Tensile Strength MPa | Elongation min. % | Impact Resistance min.[J] |
| --- | --- | --- | --- | --- |
|  | Thickness ＜16 mm | Thickness ≥16mm |  | Thickness ＜5mm | Thickness 5-16mm | Thickness ≥16mm |  |
| SS400 | 245 | 235 | 400-510 | 21 | 17 | 21 | - |

ICE steel is the professional Chinese steel exporter. We can offer you SS400 sheet, SS400 Cross Reference, SS400 Schematic, SS400 Distributor, SS400 Equivalent, SS400 Application Note, SS400 Data Sheet, SS400 component, SS400 Fiche Technique, SS400 Circuit, SS400 steel sheet, SS400 steel price. SS400 steel supplier, SS400 steel manufacturer