JIS G3131 SPHE steel plate/sheet for stamping and cold forming steels
JIS G3131 SPHE steel plate/sheet,SPHE steel plate/sheet, under JIS standard, JIS G3131 SPHE steel plate/sheet for stamping and cold forming steels,SPHE steel supplier/Chinese supplier, SPHE steel price,SPHE steel manufacturer.

SPHE steel plate/sheet is in JIS G 3131 standard. It's grade Number is 1.0398. The equal material of SPHE is: DIN 1614 RRSTW23,ASTM-SAE A621DQ-SAE1008,EN 10111 DD12.

| SPHE JIS G 3131 Number: 1.0398 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | - |
|  | DIN1614 | RRSTW23 |
|  | NFA 36-301 | - |
|  | EN 10111 | DD12 |
|  | ASTM-SAE | A621DQ-SAE1008 |
|  | UNE36.093 | - |

Main chemical composition in JIS G3131 SPHE steel: Carbon:max 0.10, Manganese max 0.50, Sulphur max 0.035, Phosphorus max 0.030. More detailed information, please refer to the flowing table: 
Chemical analysis -% by mass*

| Symbol | Chemical composition |
| --- | --- |
|  | Cmax | Mn max | P max | S max |
| SPHE | 0.10 | 0.50 | 0.030 | 0.035 |

JIS G3131 SPHE steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.SPHE tensile strength is around 270 MPa. (different min strength point at the different thickness.) More detailed information about JIS G3131 SPHE steel Mechanical Properties , please refer to the following table:
Mechanical properties

| Symbol | Tensile strength N/mm2 min | Elongation% min | Tensile test piece | Bendability |
| --- | --- | --- | --- | --- |
|  |  | ≥1.2 <1.6mm | ≥1.6 <2mm | ≥2 <2.5mm | ≥2.5 <3.2mm | ≥3.2 <4mm | ≥4mm |  | Bending angle | Inside Radius | Test piece |
|  |  |  |  |  |  |  |  |  |  | <3.2mm | ≥3.2 mm |  |
| SPHE | 270 | 31 | 33 | 35 | 37 | 39 | 41 | No.5 in rolling direction | - | - | - | No.3 in rolling direction |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like JIS G3131 SPHE steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products JIS G3131 SPHE steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.