JIS3101 SS490 low alloy steel

Key words : 
SS490 steel plate, JIS3101 SS490 steel plate, under JIS3101 standard, we can regard SS490 steel plate as low alloy steel
SS490 steel plate is one mainly of low alloy steel, SS490 steel plate is alloy steel under the JIS3101 standard which is equal to DIN17100:St52-3,JIS3101:S355JR,BS:50B and UNI7070:Fe510B 
Equivalent grade : 
SS490 steel plate/sheet is in JIS3101 standard.The equal material of SS490 is: JIS3101:1990 FE 510 B, DIN17100 ST52-3, NFA 35-501 E36-2, ASTM A572GR50,UNI7070 FE 510 B .

| SS490/SM490A JIS3101 | Comparison of steel grades |
| --- | --- |
|  | JIS3101:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | ASTM | A572GR50 |
|  | EN 10025-2 | S355JR |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

JIS3101 SS490 steel Chemical Composition 
 
Main chemical composition in JIS3101 SS490 steel :Silicium max 0.55 Manganese max 1.6, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

JIS3101 SS490 steel Mechanical Properties

JIS3101 SS490 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about JIS3101 SS490 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrength Rm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you SS490 sheet, SS490 Cross Reference, SS490 Schematic, SS490 Distributor, SS490 Equivalent, SS490 Application Note, SS490 Data Sheet, SS490 component, SS490 Fiche Technique, SS490 Circuit, SS490 steel sheet, SS490 steel price. SS490 steel supplier, SS490 steel manufacturer.