JIS3106 SM400A/B/C carbon and low alloy steel

Key words : 
SM400A/B/C steel plate, JIS3106 SM400A/B/C steel plate, under JIS3106 standard, we can regard SM400A/B/C steel plate as Carbon steel
SM400A/B/C steel plate is one mainly of Carbon steel, SM400A/B/C steel plate is a structural steel grade which be used in riveted, bolted, or welded construction of bridges and buildings.It is identical to DIN:St37-3U,BS:40C,JIS3106:S235J0 and Fe360C and etc 
Equivalent grade : 
SM400A/B/C steel plate/sheet is in JIS3106 standard. The equal material of SM400A/B/C is: JIS3106:1990 FE 360C, DIN17100 ST37-3U, NFA 35-501 E24-3, BS1449 40C - EN 10025-2  S235J0,UNI7070 FE 360 C .

| SM400B JIS3106 | Comparison of steel grades |
| --- | --- |
|  | JIS3106:1990 | FE E 360 C |
|  | DIN17100 | ST37-3U |
|  | NFA 35-501 | E24-3 |
|  | BS1449 | 40C |
|  | EN 10025-2 | S235J0 |
|  | UNI7070 | FE 360 C |

JIS3106 SM400A/B/C steel Chemical Composition 
 
Main chemical composition in JIS3106 SM400A/B/C steel : Manganese max 1.4, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

JIS3106 SM400A/B/C steel Mechanical Properties

JIS3106 SM400A/B/C steel plate/sheet for carbon and low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about JIS3106 SM400A/B/C steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm[N/mm2]transv. | Fracture Elongation [%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you SM400A/B/C sheet, SM400A/B/C Cross Reference, SM400A/B/C Schematic, SM400A/B/C Distributor, SM400A/B/C Equivalent, SM400A/B/C Application Note, SM400A/B/C Data Sheet, SM400A/B/C component, SM400A/B/C Fiche Technique, SM400A/B/C Circuit, SM400A/B/C steel sheet, SM400A/B/C steel price. SM400A/B/C steel supplier, SM400A/B/C steel manufacturer.