JIS3106 SM490A/B/C Carbon and low alloy steel 
Key words : 
SM490A/B/C steel plate, JIS3106 SM490A/B/C steel plate, under JIS3106 standard, we can regard SM490A/B/C steel plate as low alloy steel SM490A/B/C steel plate is one mainly of low alloy steel, SM490A/B/C Steel plate is alloy steel under the JIS3106 standard which is equal to DIN17100:St52-3,EN 10025-2:S355JR,BS:50B and UNI7070:Fe510B

Equivalent grade : 
SM490A/B/C steel plate/sheet is in JIS3106 standard. The equal material of SM490A/B/C is: JIS3106:1990 FE 510 B, DIN17100 ST52-3, NFA 35-501 E36-2, EN 10025-2 S355JR - ASTM A572GR50,UNI7070 FE 510 B .

| SS490/SM490A JIS3106 | Comparison of steel grades |
| --- | --- |
|  | JIS3106:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | ASTM | A572GR50 |
|  | EN 10025-2 | S355JR |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

JIS3106 SM490A/B/C steel Chemical Composition % : 
 
Main chemical composition in JIS3106 SM490A/B/C steel :Silicium max 0.55 Manganese max 1.6, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

JIS3106 SM490A/B/C steel Mechanical Properties

JIS3106 SM490A/B/C steel plate/sheet for carbon and low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about JIS3106 SM490A/B/C steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you SM490A/B/C sheet, SM490A/B/C Cross Reference, SM490A/B/C Schematic, SM490A/B/C Distributor, SM490A/B/C Equivalent, SM490A/B/C Application Note, SM490A/B/C Data Sheet, SM490A/B/C component, SM490A/B/C Fiche Technique, SM490A/B/C Circuit, SM490A/B/C steel sheet, SM490A/B/C steel price. SM490A/B/C steel supplier, SM490A/B/C steel manufacturer.