JISG SS 500 steel plate/sheet for general Construction steels
Key words :
JISG SS 500 steel plate/sheet, JISG SS 500 steel plate/sheet, under JISG standard, we can regard SS 500 steel plate/sheet for general Construction steels. JISG SS 500 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of JISG SS 500 steel.
Equivalent grade : 
SS 500 steel plate/sheet is in JISG standard. The comparison of steel grades is: JISG:1990 SS500，DIN17100 ST50-2, NFA 35-501 A50-2,BS1449,UNI7070 FE 490.

| SS 500 JISG Number: 1.0050 | Comparison of steel grades |
| --- | --- |
|  | JISG :1990 | SS 500 |
|  | DIN17100 | ST50-2 |
|  | NFA 35-501 | A50-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 490 |

SS 500 steel Chemical analysis
Main chemical composition in JISG SS 500 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | - | - | - | - | 0.045 | 0.045 | 0.012 |

SS 500 steel Mechanical properties 
JISG SS 500 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about JISG SS 500 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 295 285 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 490-600 470-610 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 11 12 13 14 18 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.