LR FH32, LR FH32 steel grade, LR FH32 steel plate, LR FH32 steel sheet, LR FH32 shipbuilding steel price,LR FH32 steel supplier and manufacturer.

LR FH32 shipbuilding Steel Description:
LR FH32 steel is a kind of  hot rolled high tensile strength steel. LR FH32 steel can achieve the impact toughness at Celsius degree -60°. The LR FH 32 grade steel plates have yield strength of 45,500 psi (315 MPa), and ultimate tensile strength of 64,000 - 85,000 psi (440-590 MPa). All the LR FH32 shipbuilding Steel offered by Ice steel can be certificated by Lloyd’s Register of Shipping (LR).

LR FH32 Shipbuilding Steel Application:
LR FH32 Shipbuilding steel plates can be used for producing container and bulk cargo vessels as well as cruise ships, ferries and yachts.LR FH32 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components.

LR FH32 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

LR FH32 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LR Grade FH32 | 0.160 | 0.1-0.5 | 0.90-1.6 | 0.025 | 0.025 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % | N % |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.800 | 0.020 | 0.009 |  |  |

LR FH32 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| LR Grade FH32 | 8mm-50mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 34J |
|  | 51mm-70mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 41J |
|  | 71mm-100mm | Min 315Mpa | 440-590Mpa | 22% | -60 | 50J |
| The min impact energy is longitudinal energy |

Ice steel is a professional LR FH32 shipbuilding steel supplier and exporter. LR FH32 shipbuilding steel plates and steel sheets provided by Ice steel have been exported to worldwide shipyard and ship building company. We have steel mill for manufacturing LR Grade FH32 steel.If you have any needs in LR FH32 steel plate price, please feel free to contact us.