LR FH40, LR FH40 steel grade, LR FH40 steel plate, LR FH40 steel sheet, LR FH40 shipbuilding steel price,LR FH40 steel supplier and manufacturer.

LR FH40 shipbuilding Steel Description:
LR FH40 steel is a kind of  hot rolled high tensile strength steel. The LR FH40 grade steel plates have yield strength of 56,500 psi (390 MPa), and ultimate tensile strength of 74,000 - 94,500 psi (510-650 MPa). LR FH40 steel can achieve the impact toughness at Celsius degree -60°. All the LR FH40 shipbuilding Steel offered by Ice steel can be certificated by Lloyd’s Register of Shipping (LR).

LR FH40 Shipbuilding Steel Application:
LR FH40 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components.

LR FH40 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

LR FH40 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LR Grade FH40 | 0.160 | 0.1-0.5 | 0.90-1.6 | 0.025 | 0.025 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % | N% |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.800 | 0.020 | 0.009 |  |  |

LR FH40 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| LR Grade FH40 | 8mm-50mm | Min 390Mpa | 510-650Mpa | 20% | -60 | 34J |
|  | 51mm-70mm | Min390Mpa | 510-650Mpa | 20% | -60 | 41J |
|  | 71mm-100mm | Min 390Mpa | 510-650Mpa | 20% | -60 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. has many years experience in making every grade shipbuilding steel. We have good quality LR FH40 steel plates for sale.ICE Steel is a very good LR FH40 steel exporter too. Our steel plates and steel sheets have been exported to worldwide shipyard and ship building company.If you have any needs in LR Grade FH40 steel plate price, please feel free to contact us.