NBNA21201 A 590-1,2 steel plate/sheet for general Construction steels
Key words :
NBNA21201 A 590-1,2 steel plate/sheet,NBNA21201 A 590-1,2 steel plate/sheet, under NBNA21201 standard, we can regard A 590-1,2 steel plate/sheet for general Construction steels.NBNA21201 A 590-1,2 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of NBNA21201 A 590-1,2 steel. A 590-1,2 steel is according to NBNA21201 standard and it is equivalent to DIN17100:St60-2,NFA:A60-2 and UNI7070:Fe590 steel grades.
Equivalent grade : 
NBNA21201 A 590-1,2 steel plate/sheet is in NBNA21201 standard. The comparison of steel grades is: NBNA21201:1990 A 590-1,2，DIN17100 ST60-2, NFA 35-501 A60-2,BS1449,UNI7070 FE 590.

| A 590-1,2 NBNA21201 Number: 1.0060 | Comparison of steel grades |
| --- | --- |
|  | NBNA21201:1990 | FE 590-2 |
|  | DIN17100 | ST60-2 |
|  | NFA 35-501 | A60-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 590 |

A 590-1,2 steel Chemical analysis
Main chemical composition in NBNA21201 A 590-1,2 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical analysis -% by mass of A 590-1,2 steel Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A 590-1,2 | - | - | - | - | 0.045 | 0.045 | 0.012 |

A 590-1,2 steel Mechanical properties 
NBNA21201 A 590-1,2 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about NBNA21201 A 590-1,2 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 335 325 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 590-770 570-710 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 7 8 9 10 14 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.