NBNA21201 A 690-1,2 steel plate/sheet for general Construction steels
Key words :
NBNA21201 A 690-1,2 steel plate/sheet,NBNA21201 A 690-1,2 steel plate/sheet, under NBNA21201 standard, we can regard A 690-1,2 steel plate/sheet for general Construction steels.NBNA21201 A 690-1,2 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of EN A 690-1,2 steel. A 690-1,2 steel is according to NBNA21201 standard and it is equivalent to EN:Fe690-2,DIN17100:St70-2,NFA: A70-2 and NBNA21201:E360 steel grades.
Equivalent grade : 
NBNA21201 A 690-1,2 steel plate/sheet is in NBNA21201 standard. The comparison of steel grades is: NBNA21201 :1990 A 690-1,，DIN17100 ST60-2, NFA 35-501 A60-2,BS1449,UNI7070 FE 590

| A 690-1,2 NBNA21201 | Comparison of steel grades |
| --- | --- |
|  | NBNA21201:1990 | A 690-1,2 |
|  | DIN17100 | ST70-2 |
|  | NFA 35-501 | A70-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 690 |

A 690-1,2 steel Chemical analysis -% by mass* 
Main chemical composition in NBNA21201 A 690-1,2 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A 690-1,2 | - | - | - | - | 0.045 | 0.045 | 0.012 |

A 690-1,2 steel Mechanical properties 
NBNA21201 A 690-1,2 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about NBNA21201 A 690-1,2 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 360 355 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 690-900 670-830 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 4 5 6 7 10 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.