NFA 36-301 E 420 FP steel plate/sheet for fine-grain structural steel

Key words: E 420 FP steel plate/sheet, NFA 36-301 E 420 FP steel plate/sheet, E 420 FP steel plate/sheet supplier/Chinese supplier, E 420 FP steel plate/sheet mechanical property, E 420 FP steel plate/sheet price.

NFA 36-301 E 420 FP steel equivalent grade:
E 420 FP steel plate/sheet is in NFA 36-301 standard, the grade number is 1.8912. The equivalent material of E 420 FP steel are UNE36081 AE 420 KT, EN 10111 S420N, DIN17102 T StE 420.

| E420FP NFA36-301 MATERIAL# 1.8912 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 420 KT |
|  | EN 10111 | S420N |
|  | UN | - |
|  | DIN17102 | T StE 420 |
|  | BS4360 | - |

NFA 36-301 E 420 FP steel chemical composition %:
Main chemical composition in E 355 R steel is carton max 0.20, silicon max 0.60, manganese max 1.00-1.70, phosphorus max 0.025, Sulphur max 0.020, chromium max 0.30. More detailed information about E 420 FP steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.60 | 1.00-1.70 | 0.025 | 0.020 | 0.55 | 0.30 | 0.80 | 0.20 | 0.05 | 0.02 |

NFA 36-301 E 420 FP steel mechanical property:
E420FP steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, which with a minimum fracture elongation of 19% and the tensile strength of E420FP is 520 to680 MPa.

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 420 400 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t≥ 3mm |  | 520-680 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 19 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of NFA 36-301 E 420 FP steel are available, so if need, welcome to contact ICE steel sales team.