NFA 36201 E 460 FP steel plate/sheet for High Yield Steel

Key words: E 460 FP steel plate/sheet, NFA 36201 E 460 FP steel plate/sheet, E 460 FP steel plate/sheet supplier/Chinese supplier, E 460 FP steel plate/sheet price, E 460 FP steel plate/sheet mechanical property.

NFA 36201 E 460 FP steel chemical composition %:
Main chemical composition in NFA 36201 E 460 FP steel is carton max 0.20, silicon max 0.60, manganese max 1.70, phosphorus max 0.025, Sulphur max 0.015. More detailed information about E 460 FP steel, please refer to the down table:

| Element | P460NH Max % | Element | P460NH max % |
| --- | --- | --- | --- |
| C | 0.20 | Cr | 0.30 |
| Si | 0.60 | Cu | 0.70 |
| Mn | 1.10-1.70 | Mo | 0.10 |
| P | 0.025 | Nb | 0.05 |
| S | 0.015 | Ni | 0.80 |
| AL | 0.020 | Ti | 0.03 |
| N | 0.025 | V | 0.20 |

NFA 36201 E 460 FP steel mechanical property:
E 460FP steel plate is one of the mainly High Yield steel, Steel sheet E 460FP shall be at minus 20 centi degree on transverse at minimum 30 J impacting energy.

| Grade | Type | Thickness | Yield Strength | Tensile Strength | Elongation | Impact Energy |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | (mm) | MPa (min) | MPa | % (min) | (KV J) (min) |
|  |  |  |  |  |  | -20 degree |
| E460FP | Normalized | ≤ 16 | 460 | 570-720 | 17 | 30 |
|  |  | 16> to ≤40 | 445 | 570-720 | 17 | 30 |
|  |  | 40> to ≤60 | 430 | 570-720 | 17 | 30 |
|  |  | 60> to ≤100 | 400 | 540-710 | 17 | 30 |
|  |  | 100> to ≤150 | 400 | 540-710 | 17 | 30 |
|  |  | 150> to ≤250 | 400 | 540-710 | 17 | 30 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of NFA 36201 E 460 FP steel are available, so if need, welcome to contact ICE steel sales team.