NK AH40, NK AH40 steel plate, NK AH40 steel plate, NK AH40 steel sheet, NK AH40 shipbuilding steel price,NK AH40 steel supplier and manufacturer.

NK AH40 shipbuilding Steel Description:
NK AH40 steel is a kind of  high tensile strength shipbuilding steel. All NK AH40 steels are standard hot rolled carbon steels. All of these steels have been engineered to be optimal long-lived shipbuilding steels. Higher-strength NK shipbuilding steel comes in 12 grades of 3 strengths, AH40 is one of the grades.

NK AH40 Shipbuilding Steel Application:
NK AH40 Shipbuilding steel plates are mainly used for making the offshore oil drilling platform, the hull of ship building and ship repairing, the platform pipe joints and other components.

NK AH40 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

NK AH40 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NK Grade AH40 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

NK AH40 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| NK Grade AH40 | 8mm-50mm | Min 390Mpa | 510-650Mpa | 20% | 0 | 34J |
|  | 51mm-70mm | Min390Mpa | 510-650Mpa | 20% | 0 | 41J |
|  | 71mm-100mm | Min 390Mpa | 510-650Mpa | 20% | 0 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. is a professional NK AH40 steel manufacturer and exporter. Our NK AH40 steel plates and steel sheets have been exported to worldwide shipyard and ship building company.If you have any needs in NK Grade AH40 steel plate price, please feel free to contact us.