NK EH32, NK EH32 steel grade, NK EH32 steel plate, NK EH32 steel sheet, NK EH32 shipbuilding steel price,NK EH32 steel supplier and manufacturer.

NK EH32 shipbuilding Steel Description:
All NK steels are standard carbon steels. As with other grades of steel, they have a specific gravity of 7.8. Higher-strength NK shipbuilding steel comes in 12 grades of 3 strengths, EH32 is one of the grades.The NK EH 32 grade steel plates have yield strength of 45,500 psi (315 MPa), and ultimate tensile strength of 64,000 - 85,000 psi (440-590 MPa).

NK EH32 Shipbuilding Steel Application:
NK EH32 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components.

NK EH32 Steel Grade Specification:
Thickness: 4mm to 260mm
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm

NK EH32 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NK Grade EH32 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

NK EH32 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| NK Grade EH32 | 8mm-50mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 34J |
|  | 51mm-70mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 38J |
|  | 71mm-100mm | Min 315Mpa | 440-590Mpa | 22 | -40 | 46J |
| The minimum impact energy is longitudinal energy |

ICE Steel has been working in the steel industry for many years. Ice steel is a professional NK EH32 shipbuilding steel supplier and exporter. NK EH32 shipbuilding steel plates and steel sheets provided by Ice steel have been exported to worldwide shipyard and ship building company. If you have any needs in NK EH32 steel plate price, please feel free to contact us.