NK EH36, NK EH36 steel grade, NK EH36 steel plate, NK EH36 steel sheet, NK EH36 shipbuilding steel price,NK EH36 steel supplier and manufacturer.

NK EH36 Shipbuilding Steel Description:
NK EH36 steel is a kind of  high tensile strength marine steel. All of these steels have been engineered to be optimal long-lived shipbuilding steels.As with other grades of steel, they have a specific gravity of 7.8. The NK EH36 grades have yield strength of 51,000 psi (355 MPa), and ultimate tensile strength of 71,000 - 90,000 psi (490-620 MPa).

NK EH36 Shipbuilding Steel Application:
NK EH36 Shipbuilding steel plates can be used for producing container and bulk cargo vessels as well as cruise ships, ferries and yachts. NK EH36 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components.

NK EH36 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

NK EH36 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NK Grade EH36 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

NK EH36 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| NK Grade EH36 | 8mm-50mm | Min 355Mpa | 490-620Mpa | 21% | -40 | 34J |
|  | 51mm-70mm | Min 355Mpa | 490-620Mpa | 21% | -40 | 41J |
|  | 71mm-100mm | Min 355Mpa | 490-620Mpa | 21% | -40 | 50J |
| The min impact energy is longitudinal energy |

BeiJing ICE iron and steel co., Ltd. is a professional company for offering NK EH36 shipbuilding steel. ICE Steel is a NK EH36 steel exporter too. The NK EH36 shipbuilding steel plates and sheets we made have been exported to many countries for ship building using.If you have any needs in NK Grade EH36 steel plate price, please feel free to contact us.