EN 10028-2 P235 GH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P235 GH steel plate/sheet, EN 10028-2 P235 GH steel plate/sheet, EN 10028-2 P235 GH steel plate/sheet for Boilers and Pressure Vessel steel, P235 GH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-2 steel plate for Boilers and Pressure Vessel using, P235 GH steel supplier/Chinese supplier, P235 GH steel price...

Equivalent grade :
P235 GH steel plate/sheet is in EN10028-2 standard, It's grade Number is 1.0345. The equal material of P235 GH steel is: DIN 17155 HI, NFA 36-205 A37 CP, UNI 5869 Fe360 1KW,BS 1501 161 Gr. 360 / 164 Gr. 360, UNE 36087 A37 RCI, ASTM A 285 Gr. C-A 414 Gr. C / A 516 Gr. 55, JIS G3115 SPV 24

| P235GH EN 10028-2 Number:1.0345 | Comparision of steel grades |
| --- | --- |
|  | DIN 17155 | HI |
|  | NFA 36-205 | A 37 CP |
|  | UNI 5869 | Fe 360 1KW |
|  | BS 1501 | 161 Gr. 360 / 164 Gr. 360 |
|  | UNE 36087 | A 37 RCI |
|  | ASTM | A 285 Gr. C-A 414 Gr. C / A 516 Gr. 55 |
|  | JIS G3115 | SPV 24 |

EN10028-2 P235 GH steel Chemical Composition % : 
Main chemical composition in EN10028-2 P235 GH steel: Carbon Max 0.16 , Manganese Max 0.35, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.35, More detailed information, please refer to the flowing table:

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P235GH | 0.16 | 0.35 | 0.60-1.20 | 0.025 | 0.015 | 0.012 | 0.02 | 0.3 | 0.03 | 0.08 | 0.3 | 0.02 | 0.03 | 0.02 |

EN10028-2 P235 GH steel Mechanical Properties 
P235 GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 170 - 235 MPa (there is different min strength point at the different thickness.) P235 GH tensile strength is from 350MPa to 480MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P235 GH  steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P235GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 235 | 360-480 | 24 | 27 | 34 | 40 |
|  |  |  | 225 | 360-480 | 24 | 27 | 34 | 40 |
|  |  |  | 215 | 360-480 | 24 | 27 | 34 | 40 |
|  |  |  | 200 | 360-480 | 24 | 27 | 34 | 40 |
|  |  |  | 185 | 350-480 | 24 | 27 | 34 | 40 |
|  |  |  | 170 | 350-480 | 24 | 27 | 34 | 40 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.