EN 10028-2 P265GH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P265GH steel plate/sheet, EN 10028-2 P265GH steel plate/sheet, EN 10028-2 P265GH steel plate/sheet for Boilers and Pressure Vessel steel, P265GH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-2 steel plate for Boilers and Pressure Vessel using, P265GH steel supplier/Chinese supplier, P265GH steel price...

Equivalent grade :
P265GH steel plate/sheet is in EN10028-2 standard, It's grade Number is 1.0425. The equal material of P265GH steel is: DIN 17155 HII, NFA 36-205 A42 CP, UNI 5869 Fe410 1KW,BS 1501 161 Gr. 400 / 164 Gr. 400, UNE 36087 A42 RCI, ASTM A 414 Gr. E / A 516 Gr. 60

| P265GH EN 10028-2 Number:1.0425 | Comparision of steel grades |
| --- | --- |
|  | DIN 17155 | HII |
|  | NFA 36-205 | A 42 CP |
|  | UNI 5869 | Fe 410-1KW |
|  | BS 1501 | 161 Gr.400/164 Gr.400/224 Gr. 400 |
|  | UNE 36087 | A 42 RCI |
|  | ASTM | A 414 Gr. E / A 516 Gr. 60 |

EN10028-2 P265GH steel Chemical Composition % : 
Main chemical composition in EN10028-2 P265GH steel: Carbon Max 0.20, Manganese from 0.80 to 1.40, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

| Grade | C. max | Mn. max | S. max | N max | Cu max | Nb max | Ti. max | Si. max | P. max | AL. max | Cr. max | Mo. max | Ni. max | Vi max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P265GH | 0.20 | 0.80-1.40 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

EN10028-2 P265GH steel Mechanical Properties 
P265GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 185 - 265 MPa (there is different min strength point at the different thickness.) P265GH tensile strength is from 390MPa to 530MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P265GH steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P265GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 265 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 255 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 245 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 215 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 200 | 400-530 | 22 | 27 | 34 | 40 |
|  |  |  | 185 | 390-530 | 22 | 27 | 34 | 40 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.