EN 10028-3 P275NH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P275NH steel plate/sheet, EN 10028-3 P275NH steel plate/sheet, EN 10028-3 P275NH steel plate/sheet for Boilers and Pressure Vessel steel, P275NH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-3 steel plate for Boilers and Pressure Vessel using, P275NH steel supplier/Chinese supplier, P275NH steel price...

Equivalent grade :
P275NH steel plate/sheet is in EN 10028-3 standard. The equal material of P275NH steel is: DIN 17135 WSt 285, NFA 36-205  A 42 CP,AP,FP

| P275NH EN 10028-2 | Comparison of steel grades |
| --- | --- |
|  | EU 113 | - |
|  | NBN629 | - |
|  | DIN 17102 | WSt 285 |
|  | NFA36205 | A 42 CP,AP,FP |

EN 10028-3 P275NH steel Chemical Composition % : 
Main chemical composition in EN 10028-3 P275NH steel: Carbon Max 0.16, Manganese from 0.08 to 1.50, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

EN 10028-3 P275NH steel  steel Chemical Composition %

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P275NH | 0.16 | 0.40 | 0.80-1.50 | 0.025 | 0.015 | 0.012 | 0.020 | 0.300 | 0.30 | 0.08 | 0.50 | 0.05 | 0.03 | 0.05 |

EN 10028-3 P275NH steel Mechanical Properties 
P275NH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 215- 275 MPa (there is different min strength point at the different thickness.) P275NH tensile strength is from 350MPa to 510MPa. (different min strength point at the different thickness.) More detailed information about EN 10028-3 P275NH steel Mechanical Properties , please refer to the following table:

| Grade | Thickness ( mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- |
| P275NH | ≤ 16 | 275 | 390 to 510 | 24 |
|  | 16＜t ≤40 | 265 | 390 to 510 | 24 |
|  | 40＜t ≤60 | 255 | 390 to 510 | 24 |
|  | 6＜t ≤100 | 235 | 370 to 490 | 23 |
|  | 100＜t ≤150 | 225 | 360 to 480 | 23 |
|  | 150＜t ≤250 | 215 | 350 470 | 23 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.