EN 10028-2 P295GH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P295GH steel plate/sheet, EN 10028-2 P295GH steel plate/sheet, EN 10028-2 P295GH steel plate/sheet for Boilers and Pressure Vessel steel, P295GH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-2 steel plate for Boilers and Pressure Vessel using, P295GH steel supplier/Chinese supplier, P295GH steel price...

Equivalent grade :
P295GH steel plate/sheet is in EN10028-2 standard, It's grade Number is 1.0481. The equal material of P295GH steel is: DIN 17155 17Mn4, NFA 36-205 A48 CP, UNI 5869 Fe460 1KW,BS 1501 224 Gr. 490, UNE 36087 A47 RCI, ASTM A 414 Gr. F / A 516 Gr. 65, JIS G3115 SPV 32.

| P295GH EN 10028-2 Number:1.0481 | Comparision of steel grades |
| --- | --- |
|  | DIN 17155 | 17 Mn 4 |
|  | NFA 36-205 | A 48 CP |
|  | UNI 5869 | Fe 460-1KW |
|  | BS 1501 | 224 Gr. 490 |
|  | UNE 36087 | A 47 RCI |
|  | ASTM | A 414 Gr. F / A 516 Gr. 65 |
|  | JIS G3115 | SPV 32 |

EN10028-2 P295GH steel Chemical Composition % : 
Main chemical composition in EN10028-2 P295GH steel: Carbon from 0.08 to 0.20, Manganese from 0.90 to 1.50, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn. % | S. max | N max | Cu max | Nb max | Ti. max | Si. max | P. max | AL. max | Cr. max | Mo. max | Ni. max | Vi max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P295GH | 0.08-0.20 | 0.90-1.50 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

EN10028-2 P295GH steel Mechanical Properties 
P295GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 220- 295 MPa (there is different min strength point at the different thickness.) P295GH tensile strength is from 430MPa to 580MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P295GH steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P295GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 295 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 290 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 285 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 260 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 235 | 440-570 | 21 | 27 | 34 | 40 |
|  |  |  | 220 | 430-570 | 21 | 27 | 34 | 40 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.