EN 10028-2 P355GH steel plate/sheet for Boilers and Pressure Vessels
Key words :
P355GH steel plate/sheet, EN 10028-2 P355GH steel plate/sheet, EN 10028-2 P355GH steel plate/sheet for Boilers and Pressure Vessel steel, P355GH steel plate/sheet for Boilers and Pressure Vessel, EN 10028-2 steel plate for Boilers and Pressure Vessel using, P355GH steel supplier/Chinese supplier, P355GH steel price...

Equivalent grade :
P355GH steel plate/sheet is in EN10028-2 standard, It's grade Number is 1.0473. The equal material of P355GH steel is: DIN 17155 19 Mn 6, NFA 36-205 A52 CP, UNI 5869 Fe510 1KW, UNE 36087 A52 RCI, ASTM A 414 Gr. G, JIS G3115 SPV 36.

| P355GH EN 10028-2 Number:1.0473 | Comparision of steel grades |
| --- | --- |
|  | DIN 17155 | 19 Mn 6 |
|  | NFA 36-205 | A 52 CP |
|  | UNI 5869 | Fe 510-1KW |
|  | BS 1501 | - |
|  | UNE 36087 | A 52 RCI |
|  | ASTM | A 414 Gr. G |
|  | JIS G3115 | SPV 36 |

EN10028-2 P355GH steel Chemical Composition % : 
Main chemical composition in EN10028-2 P355GH steel: Carbon from 0.10 to 0.22, Manganese from 1.10 to 1.70, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.60, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn. % | S. max | N max | Cu max | Nb max | Ti. max | Si. max | P. max | AL. max | Cr. max | Mo. max | Ni. max | Vi max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P355GH | 0.10-0.22 | 1.10-1.70 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.60 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

EN10028-2 P355GH steel Mechanical Properties 
P355GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 280- 355 MPa (there is different min strength point at the different thickness.) P355GH tensile strength is from 470MPa to 650MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P355GH steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P355GH | Normalized | ≤16 | 355 | 510-650 | 20 | 27 | 34 | 40 |
|  |  | 16>to≤40 | 345 | 510-650 | 20 | 27 | 34 | 40 |
|  |  | 40>to≤60 | 335 | 460-580 | 20 | 27 | 34 | 40 |
|  |  | 60>to≤100 | 315 | 490-630 | 20 | 27 | 34 | 40 |
|  |  | 100>to≤150 | 295 | 480-630 | 20 | 27 | 34 | 40 |
|  |  | 150>to≤250 | 280 | 470-630 | 20 | 27 | 34 | 40 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.