RINA AH32, RINA AH32 steel grade, RINA AH32 steel plate, RINA AH32 steel sheet, RINA AH32 shipbuilding steel price,RINA AH32 steel supplier and manufacturer.

RINA AH32 shipbuilding Steel Description:
RINA AH32 steel is a kind of  hot rolled high tensile strength steel. As with other grades of steel, RINA AH32 steel has a specific gravity of 7.8. Higher-strength RINA shipbuilding steel comes in 12 grades of 3 strengths, AH32 is one of the grades. The RINA AH 32 grade steel plates have yield strength of 45,500 psi (315 MPa), and ultimate tensile strength of 64,000 - 85,000 psi (440-590 MPa). All the RINA AH32 shipbuilding Steel offered by Ice steel can be certificated by Registro Italiano Navale (RINA).

RINA AH32 Shipbuilding Steel Application:
RINA AH32 Shipbuilding steel plates are mainly used for making the hull of ship building and ship repairing, the offshore oil drilling platform, the platform pipe joints and other components. RINA AH32 Shipbuilding steel plates also can be used for producing container and bulk cargo vessels as well as cruise ships, ferries and yachts.

RINA AH32 Steel Grade Specification:
Thickness: 4mm to 260mm, 
Width: 1200mm to 4000mm
Length: 3000mm to 18000mm.

RINA AH32 Shipbuilding Steel Chemical Composition:

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RINA Grade AH32 | 0.180 | 0.1-0.5 | 0.90-1.6 | 0.035 | 0.035 | 0.05-0.10 | 0.015 | 0.200 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.350 | 0.080 | 0.02-0.05 | 0.400 | 0.020 |  |  |  |

RINA AH32 Grade Ship Steel Mechanical Properties:

| Grade | Thickness(mm) | MinYield(Mpa) | Tensile(Mpa) | Elongation (%) | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| RINA Grade AH32 | 8mm-50mm | Min 315Mpa | 440-590Mpa | 22% | - | 34J |
|  | 51mm-70mm | Min 315Mpa | 440-590Mpa | 22% | - | 38J |
|  | 71mm-100mm | Min 315Mpa | 440-590Mpa | 22% | - | 46J |
| The min impact energy is longitudinal energy |

RINA AH32 shipbuilding steel plates and steel sheets provided by Ice steel have been exported to worldwide shipyard and ship building company. Ice steel is a professional RINA AH32 shipbuilding steel supplier and exporter. We have steel mill for manufacturing RINA Grade AH32 steel.If you have any needs in RINA AH32 steel plate price, please feel free to contact us.